## Slide 1: Hydration of Cement
Doha M. Abdul-Razzaq Al Saffar
Al Mansour University College
Civil Engineering Department
2017

## Slide 2: Definition
It is the reaction (series of chemical reactions) of cement with water to form the binding material. In other words, in the presence of water, the silicates (C3S and
C2S) and aluminates (C3A and C4AF) form products of hydration which in time produce a firm and hard mass - the hydrated cement paste.

## Slide 4: The rates of the chemical reactions of the main compounds are different:
Aluminates
React with the water in the beginning
Affect the route of the chemical reactions at early periods of hydration.
Silicates - Affect the later stage reactions.

## Slide 5: The main hydrates of the hydration process are:
- Calcium silicates hydrate, including hydrated products of C3S, and C2S.
2 C3S + 6H→ C3S2H3 + 3 Ca(OH)2
2 C2S + 4H→ C3S2H3 + Ca(OH)2
- Tricalcium aluminate hydrate.
C3A + 6H→ C3AH6
- C4AF hydrates to tricalcium aluminate hydrate and calcium ferrite CaO.Fe2O3
in amorphous form.
Since calcium silicates (C3S and C2S) - are the main cement compounds
(occupies about 75% of cement weight) - they are responsible for the final
strength of the hardened cement paste.

## Slide 6
With time:
- The rate of hydration decreases continuously.
- The size of unhydrated cement particles decrease. For instance, after 28 days in
contact with water, grains of cement have been found to have hydrated to a
depth of only 4 μm, and 8 μm after a year.
This is due to:
1) Accumulation of hydration products around the unhydrated cement grains
which lead to prevent water from channeling to them.
2) Reduction of the amount of water either due to chemical reaction or
evaporation.
3) Reduction of the amount of cement due to reaction.

## Slide 7: The progress of hydration of cement can be determined by different means:
The measurement of the amount of Ca(OH)2 in the paste resulted from the
hydration of the silicates.
The heat evolved by hydration.
The specific gravity of the paste.
The amount of chemically combined water.
The amount of unhydrated cement present (using X-ray quantitative analysis).
Also indirectly from the strength of the hydrated paste

## Slide 8: Tricalcium Aluminate Hydrate and the Action Of Gypsum
If C3A exhausted before gypsum
The surplus gypsum → expand → become an agent assist the disruption and
deterioration of cement paste.
If gypsum exhausted before C3A
The remaining C3A begins in hydration:
C3A + 6H→C3AH6
C3AH6 is stable - cubical crystals- with high sulfate resistance.
Calcium aluminate hydrate - Be at many forms before transforming to the stable
state (C3AH6). It is probably forming hexagonal crystals (C4AH8, C4AH10.
C4AH12) before the cubical crystals.
When the hexagonal crystals expose to sulfates (inside concrete from sand
or external from soil or ground water) → react with it forming calcium
sulfoaluminate → with increase in volume, depending on the amount of
remaining aluminates and the concentration' of sulfates → crack and deteriorate
of the hardened concrete.

## Slide 9: Ettringite

## Slide 10
C4AF compound
Gypsum reacts with C4AF to form calcium sulfoaluminates and calciumsulfoferrite.’
C4AF - work as flux material and also it accelerates the hydration of silicates.
* Using The Optimum Percentage of Gypsum is Very Important Because:
- It regulates the speed of the chemical reactions in the early ages.
- Prevent the local concentration of the hydration products.
The necessary gypsum content increase with the increase of:
- C3A content in the cement.
- Alkalis content in the cement.
- Fineness of cement.

## Slide 11: Calcium Silicates Hydrate
C3S+ water→
- lime and silica ions in the solution with molecular weight of 3: 1
- Ca(OH)2 crystals
- Calcium silicate hydrate gel (tobermorite)
Hydration of C3S - take about one year or more
This initial gel form an external layer over C3S causing the delay of the reaction.
After few hours, this initial C-S-H undergo hydrolysis to form the second
product of the gel CSH. The full hydration of C3S can be expressed
approximately following equation
2 (3CaO.SiO2) + 6H2O→ 3CaO.2SiO2.3H2O + 3 Ca(OH)2

## Slide 12
C2S
There are three main crystal forms of C2S (α, β, ) but the β-form is the only
one occurred in the Portland cement and it react slowly with water.
- its reaction is slower than C3S
- The amount of Ca(OH)2 from its hydration is less.
Its formed gel is similar to that produced from C3S, but there is difference in the route of the chemical reactions between the two components
- the lime: silica during the hydration of C2S differs than that formed during the hydration of C3S.
Hydration of C2S - take more than 4 years.
The gel formed after the completion of hydration of the two components is → C3S2H3 - Tobermorite.