## Slide 1: Aggregate
Doha M. Abdul-Razzaq Al Saffar
Al Mansour University College
Civil Engineering Department
2017

## Slide 2: Porosity / Absorption of Aggregates:
Porosity or permeability of aggregates and its absorption may affect the following factors:
  The bond between aggregate and cement paste
  Resistance to freezing & thawing of concrete
  Chemical stability
  Resistance to abrasion
  Specific gravity
  Yield of concrete for a given weight of agg.

## Slide 3: 4) Bulking of Aggregates:
The free moisture content in fine agg. Results in bulking of volume.
Free moisture forms a film around each particle. This film of moisture exerts which is known as surface tension which keeps every particles away from each other. Hence no point of contact is possible between the particles & this causes the bulking of the volume.
The bulking increases with increase in moisture content upto a certain limit & beyond that the further increase in moisture content results in decrease in volume.

## Slide 4
& at a moisture content representing saturation point, the fine agg. Shows no bulking.
The following graph shows fine sand bulks more and coarse sand bulks less.
Percentage of bulking = [(h1 – h2) / h2] x 100
Bulking may affect the yield of concrete for a given cement content.

## Slide 5: Surface Moisture on fine aggregate

## Slide 6: Measurement of Moisture Content of Aggregates:
Determination of this is of vital importance in the control of the quality of concrete with respect to workability and strength.
The water content can be expressed in terms of the wt of the agg. when absolutely dry, surface dry or when wet.
Water content means the free water that held on the surface of the agg.
It can be measured by-
Drying Method, Displacement Method, Automatic Measurement, & by Electrical method.

## Slide 7: Deleterious substances in Aggregate
a. Organic impurities :
If the aggregate contain organic impunities which interfere with the chemical reactions of hydration.
Such materials are more likely to be present in sand than in coarse aggregate which is easily washed.
The organic matter found in aggregate consists usually of products of decay of vegetable matter, and appears in the form of humans or organic loam
b. Clay and other fine material :
- Clay < 0.002mm(diameter)
- Silt : is material between (2-60)mm
- Crusher dust: is a fine material form during the process of communion of rock in to crushed stone or, less frequently, of gravel in to crushed fine aggregate.
Clay may be present in aggregate in the form surface coating which interfere with the bond between aggregate and cement paste. Because good bond is essential to ensure a satisfactory strength and durability of concrete, the problem of clay coatings is an important one.

## Slide 8
It can swell, causing disruption of concrete and, if present in large quantities in a finally divided form it can disturb the process of hydration of the cement paste.
Mica should be avoided because, in presence of active chemical agents produced during the hydration of cement alteration of mice to other forms can occur, and it affects adversely the water requirement and the strength of concrete.

## Slide 9: Soundness of aggregate
This is the term used to describe the ability of aggregate to resist excessive change in volume as result of changes in physical condition lack of soundness is thus distinct from expansion from expansion caused by the chemical reactions between the aggregate and alkalis in cement .
The physical cause of large or permanent volume changes of aggregate are freezing and thawing , thermal changes of temperature above freezing , and alternating wetting and drying .
Aggregate is said to be unsound when volume changes, indused by the above causes, result in deterioration concrete.