## Slide 1: Structure of Hydrated Cement Paste
Doha M. Abdul-Razzaq Al Saffar
Al Mansour University College
Civil Engineering Department
2017

## Slide 2: Structure of hydrated cement
At any stage of hydration, the hardened paste consists of very poorly crystallized hydrates of the various compounds (calcium silicates hydrate, tricalcium aluminates hydrate and calcium ferrite), referred to collectively as gel, of crystals of Ca(OH)2 produced from the hydration of the silicates, some minor components, unhydrated cement, and the residue of the water-filled spaces in the fresh paste. These voids are called capillary pores but, within the gel itself, there exist interstitial voids, called gel pores.

## Slide 3
Hydration
Products
Unhydrated
Grain
Capillary
Porosity

## Slide 5
Capillary pores:
- cannot be viewed directly but their median size was estimated to be about 1.3 μm.
- They vary in shape and form an interconnected system randomly distributed throughout the cement paste.
- These interconnected capillary pores are mainly responsible for the permeability of the hardened cement paste and for its vulnerability to cycles of freezing and thawing.
However, hydration increases the solid content of the paste and in mature and dense pastes - the capillaries can become blocked by gel and segmented so that they turn into capillary pores interconnected solely by the gel pores.

## Slide 6
Gel pores
- The gel pores are interconnected interstitial spaces between the gel particles.
- The gel pores are much smaller than the capillary pores: Less than 2 or 3 nm in nominal diameter. This is only one order of magnitude greater than the size of molecules of water. For this reason, the vapour pressure and mobility of adsorbed water are different from the corresponding properties of free water.
- The gel pores occupy about 28 per cent of the total volume of gel (gel particles + gel pores).

## Slide 7: Water held in hydrated cement paste
- Free water – present in the capillary pores – with weak firmness, and evaporate quickly leaving the paste.
- Chemically combined water – form a definite part of the hydrated compounds.
- Gel water – present in gel pores – part of it is held by the surface force of the gel particles - It is known as the adsorbed water.

## Slide 8
A convenient division of water in the hydrated cement, necessary for investigation purposes, though rather arbitrary, is into two categories:
- Evaporable water – includes water in the capillary pores and some water in the gel pores.
- Non-evaporable water – includes nearly all chemically combined water and also some water not held by chemical bonds.
The amount of non-evaporable water increases as hydration proceeds.
In well-hydrated cement, the non-evaporable water is about 18 percent by mass of the anhydrous material; this proportion rises to about 23 percent in fully hydrated cement.