## Slide 1: Heat of hydration of cement
Doha M. Abdul-Razzaq Al Saffar
Al Mansour University College
Civil Engineering Department
2017

## Slide 2: Definition
The quantity of evolved heat when the cement hydrated completely at a given temperature – Joule/gram or calorie/gram of unhydrated cement.

## Slide 3
The hydration of cement compounds - accompanied with heat evolution, energy of up to 120 cal/g of cement being liberated.
Because the thermal conductivity of concrete is comparatively low - it acts as an insulator, and in the interior of a large concrete mass, hydration can result in a large rise in temperature. A t the same time, the exterior of the concrete mass loses some heat so that a steep temperature gradient may be established and, during subsequent cooling of the interior, serious cracking may result due to the generated stresses.
At the other extreme, the heat produced by the hydration of cement may prevent freezing of the water in the capillaries of freshly placed concrete in cold weather.

## Slide 4: The actual value of the heat of hydration depends on:
1- The chemical composition of the cement
Heat of hydration of cement = sum of the heats of hydration of the individual compounds when hydrated separately.
On an average of 500 kJ/Kg of heat is evolved during complete hydration of cement
Heat of hydration of Bogue compounds

## Slide 5
2- Ambient temperature – has great effect on the rate of heat evolution – The rate of heat evolution increase with increase in the ambient temperature.
3- Type of cement
Types of cement can be arranged in descending order with respect to their rate of heat evolution, as follows:
- Rapid hardening Portland cement.
- Ordinary Portland cement.
- Modified Portland cement.
- Sulfate resistant Portland cement.
- Low heat Portland cement.

## Slide 6
4- Fineness of cement
An increase in fineness speed up the reactions of hydration and therefore the heat evolved. It is reasonable to assume that the early rate of hydration of each compound in cement is proportional to the surface area of the cement. However, at later ages, the effect of the surface area is negligible and the total amount of heat evolved is not affected by the fineness of cement.
5- Amount of cement in the mixture
The quantity of cement in the mix also affects the total heat development: thus the richness of the mix, that is, the cement content, can be varied in order to help the control of heat development.

## Slide 7: Influence of the compound composition on properties of cement
C3S and C2S – are the most important compounds – responsible for strength.
C3S – contributes most to the strength development during the first four weeks.
C2S – influences the gain in strength from 4 weeks onwards.
At the age or about one year, the two compounds, contribute approximately equally to the ultimate strength.

## Slide 8
C3A contributes to the strength of the cement paste at one to three days, and possibly longer, but causes retrogression at an advanced age.
The role of C4AF in the development of strength of cement is not clear till now,