## Slide 1: Types of Cement
Doha M. Abdul-Razzaq Al Saffar
Al Mansour University College
Civil Engineering Department
2017

## Slide 2
The properties of cement during hydration vary according to:
Chemical composition
Degree of fineness
Types of Cement
Portland cement
Natural cement
Expansive cement
High-alumina cement

## Slide 3: Types of Portland Cement
Ordinary Portland cement – Type Ι
Modified cement - Type ΙΙ
Rapid-hardening Portland cement – Type ΙΙΙ
Low heat Portland cement – Type ΙV
Sulfate-resisting Portland cement – Type VI

## Slide 4: Ordinary Portland cement
This type of cement use in constructions when there is no exposure to sulfates in the soil or groundwater.
The chemical composition requirements are listed in Iraqi specification
L.S.F. : is limited between 0.66-1.02 Where each term in brackets denotes the percentage by mass of cement composition.
This factor is limited – to assure that the lime in the raw materials, used in the cement manufacturing is not so high, so as it cause the presence of free lime after the occurrence of chemical equilibrium. While too low a L.S.F. would make the burning in the kiln difficult and the proportion of C3S in the clinker would be too low.
Fineness – not less than 2250 cm2/gm

## Slide 5: Rapid Hardening Portland Cement
• This type develops strength more rapidly than ordinary Portland cement. The initial strength is higher , but they equalize at 2-3 months
• Setting time for this type is similar for that of ordinary Portland cement
• The rate of strength gain occur due to increase of C3S compound, and due to finer grinding of the cement clinker ( the min. fineness is 3250 cm2/g (according to IQS 5)
• Rate of heat evolution is higher than in ordinary Portland cement due to the increase in C3S and C3A, and due to its higher fineness
• Chemical composition and soundness requirements are similar to that of ordinary Portland cement.

## Slide 6: Uses
• The uses of this cement is indicated where a rapid strength development is desired (to develop high early strength, i.e. its 3 days strength equal that of 7 days ordinary Portland cement), for example:
o When formwork is to be removed for re-use
o Where sufficient strength for further construction is wanted as quickly as practicable, such as concrete blocks manufacturing, sidewalks and the places that can not be closed for a long time, and repair works needed to construct quickly.
• For construction at low temperatures, to prevent the frost damage of the capillary water.
• This type of cement does not use at mass concrete constructions.

## Slide 7: Special Types of Rapid Hardening Portland Cement A-Ultra High Early Strength Cement
The rapid strength development of this type of cement is achieved by grinding the cement to a very high fineness: 7000 to 9000 cm2/g. Because of this, the gypsum content has to be higher (4 percent expressed as SO3). Because of its high fineness, it has a low bulk density. High fineness leads to rapid hydration, and therefore to a high rate of heat generation at early ages and to a rapid strength development ( 7 days strength of rapid hardening Portland cement can be reached at 24 hours when using this type of cement). There is little gain in strength beyond 28 days.
It is used in structures where early prestressing or putting in service is of importance.

## Slide 8: Extra Rapid Hardening Portland Cement
This type prepare by grinding CaCl2 with rapid hardening Portland cement. The percentage of CaCl2 should not be more than 2% by weight of the rapid hardening Portland cement.
By using CaCl2:
• The rate of setting and hardening increase (the mixture is preferred to be casted within 20 minutes).
• The rate of heat evolution increase in comparison with rapid hardening Portland cement, so it is more convenient to be use at cold weather.
• The early strength is higher than for rapid hardening Portland cement, but their strength is equal at 90 days.
• Because CaCl2 is a material that takes the moisture from the atmosphere, care should be taken to store this cement at dry place and for a storage period not more than one month so as it does not deteriorate.

## Slide 9: Low Heat Portland Cement
Composition
It contains less C3S and C3A percentage, and higher percentage of C2S in comparison with ordinary Portland cement.
Properties
1) Reduce and delay the heat of hydration. British standard (B. S.
1370 : 1974) limit the heat of hydration of this cement by:
- 60 cal/g at 7 days age
- 70 cal/g at 28 days age
2) It has lower early strength (half the strength at 7 days age and two third the strength at 28 days age) compared with ordinary Portland cement.
3) Its fineness is not less than 3200 cm2/g

## Slide 10: Uses
It is used in mass concrete constructions: the rise of temperature in mass concrete due to progression in heat of hydration -- cause serious cracks. So it is important to limit the rate of heat evolution in this type of construction, by using the low heat cement.

## Slide 11: Sulfate- resisting Cement
It contains:
- Lower percentage of C3A and C4AF – which considers as the most affected compounds by sulfates.
- Higher percentage of silicates – in comparison with ordinary Portland cement.
- For this type of cement – C2S represents a high proportion of the silicates.
- Iraqi specification no. (6) limits – max. C3A content by 3.5%
_ min. fineness by 2500 cm2/g.

## Slide 12: Properties
- Low early strength.
- Its resulted heat of hydration is little higher than that resulted from low heat cement.
Its cost is higher than ordinary Portland cement – because of the special requirements of material composition, including addition of iron powder to the raw materials.