## Slide 1: Special Types of Cement
Doha M. Abdul-Razzaq Al Saffar
Al Mansour University College
Civil Engineering Department
2017

## Slide 2
Production
This type of cement consists of an intimate mixture of Portland cement and ground granulated blastfurnace slag.
Slag – is a waste product in the manufacture of pig iron.
Chemically, slag is a mixture of 42% lime, 30% silica, 19% alumina, 5% magnesia, and 1% alkalis, that is, the same oxides that make up Portland cement but not in the same proportions.
Portland Blastfurnace Cement

## Slide 3: Properties
- Its early strength is lower than that of ordinary cement, but their strength is equal at late ages (about 2 months).
- The requirements for fineness and setting time and soundness are similar for those of ordinary cement (although actually its fineness is higher than that of ordinary cement).
- The workability is higher than that of ordinary cement.
- Heat of hydration is lower that of ordinary cement.
- Its sulfate resistance is high.

## Slide 4: Pozzolanic Cement
This type of cement consists of an intimate mixture of Portland cement and pozzolana. American standard limit the pozzolana content by 15-40% of Pozzolanic cement.
Properties & Uses
They are similar to those of Portland blastfurnace cement.

## Slide 5: White Cement
White Portland cement is made from raw materials containing very little iron oxide (less than 0.3% by mass of clinker) and magnesium oxide (which give the grey color in ordinary Portland cement). China clay (white kaoline) is generally used, together with chalk or limestone, free from specified impurities.
- Its manufacture needs higher firing temperature because of the absence of iron element that works as a catalyst in the formation process of the clinker. In some cases kreolite (sodium-aluminum fluoride) might be added as a catalyst.
- The compounds in this cement are similar for those in ordinary Portland cement, but C4AF percentage is very low.
- Contamination of the cement with iron during grinding of clinker has also to be avoided. For this reason, instead of the usual ball mill, the expensive nickel and molybdenum alloy balls are used in a stone or ceramic-lined mill. The cost of grinding is thus higher, and this, coupled with the more expensive raw materials, makes white cement rather expensive.

## Slide 6
- It has a slightly lower specific gravity (3.05-3.1), than ordinary Portland cement.
- The strength is usually somewhat lower than that of ordinary Portland cement.
- Its fineness is higher (4000-4500 cm2/g) than ordinary Portland cement.

## Slide 7: Colored Portland Cement
It is prepared by adding special types of pigments to the Portland cement. The pigments added to the white cement (2-10% by weight of the cement) when needed to obtain light colors, while it added to ordinary Portland cement when needed to obtain dark colors.
The 28-day compressive strength is required to be not less than 90% of the strength of a pigment-free control mix, and the water demand is required to be not more than 110% of the control mix.
It is required that pigments are insoluble and not affected by light. They should be chemically inert and don't contain gypsum that is harmful to the concrete.

## Slide 8: Expansive Cement
It has the property of expanding in its early life so as to counteract contraction induced by drying shrinkage.