## Slide 1: Aggregate
Doha M. Abdul-Razzaq Al Saffar
Al Mansour University College
Civil Engineering Department
2017

## Slide 2: Grading of Aggregates:
Grading is the particle-size distribution of an aggregate as determined by a sieve analysis using wire mesh sieves with square openings.
According to ASTM
Fine aggregate - 7 standard sieves with openings from 150 μm to 9.5 mm
Coarse aggregate - 13 sieves with openings from 1.18 mm to 100 mm

## Slide 3
 | IS Sieves
 | 125 mm
 | 90 mm
Sieves for Fine | 63 mm
Aggregates | 31.5 mm
 | 16 mm
 | 8 mm
 | 4 mm
 | 2 mm
 | 1 mm
 | 0.5 mm
 | 0.25 mm
 | IS Sieves
 | 125 mm
 | 100 mm
 | 90 mm
 | 75 mm
Sieves for | 63 mm
Coarse | 50 mm
Aggregates | 37.5 mm
 | 25 mm
 | 12.5 mm
 | 9.5 mm
 | 4.75 mm
 | 2.38 mm
 | 1.19 mm
 | 0.595 mm
 | 0.297 mm
 | 0.149 mm

## Slide 4
The material is sieved through a series of sieves that are placed one above the other in order of size with the largest sieve at the top.
Dry agg. is sieved to prevent lumps.
*****
Agg.
#4
#8
#16
#30
#50
#100
Pan
Sieve shaker
Lateral & Vertical motion

## Slide 6
The particle size distribution in an aggregate sample is known as “gradation”.
Strength development of concrete depends on degree of compaction & workability together with many other factors. So, a satisfactory concrete should be compacted to max density with a reasonable work.
On the other hand, in good concrete all aggregate particles must be covered by cement paste.
The grading of aggregate must be so that the workability, density & volume stability of concrete may not be adversely affected by it.

## Slide 7
A reasonable combination of fine & coarse aggregate must be used. This can be expressed by maximum density or minimum voids concept.

## Slide 8
There are two different methods for determining the agg. grading:
Fineness Modulus (FM)
Granulometry
The grading of the particles in an agg. sample is performed by “sieve analysis”. The sieve analysis is conducted by the use of “standard test sieves”. Test sieves have square openings & their designation correspond to the sizes of those openings.
Determination of the Grading of Aggregate:

## Slide 9
Fineness Modulus (FM):
FM is a single figure which is the sum of cumulative % retained on a series of sieves having a clear opening half that of the preceeding one. Usually determined for fine agg.
FM =
Σ (% cumulative retained on each sieve)
100

## Slide 10: Physical Properties of Aggregates 1) Specific gravity:
Specific gravity is the ratio of the weight of a unit volume of material to the Weight of the same volume of water at 20º to 25ºC.
G = (Wt/V) / (Wtw/V)
Where, G – Specific Gravity
Wt – Weight of Material
V – Volume
Wtw – Weight of water

## Slide 11
Sp.Gr. is used in certain computations for concrete mix design or control work, such as, absolute volume of aggregate in concrete. It is not a measure of the quality of aggregate.
Sp.Gr.=
Weight of Agg. (WA)
Weight of an equal volume of water (VA*ρw)

## Slide 12: 2) Bulk Density
The bulk density or unit weight of an aggregate gives valuable information regarding the shape and grading of the aggregate.
It is measured by filling a container of known volume in a standard manner and weighing it.
It shows how densely the aggregate is packed when filled in a standard manner.
It is depend on size and shape of aggregates.
Higher the bulk density lower is the void content to be filled by sand and cement.

## Slide 13
It is calculated by,
Percentage voids = [(Gs - γ) / Gs] x 100
Where, Gs – Specific gravity of aggregate
γ – Bulk density in kg/lit
Reduction of Voids

## Slide 14: 3) Absorption & Moisture Condition of Aggregates:
Some of the aggregates are porous and absorptive & it will affect water – cement ratio and hence workability of concrete & durability of concrete.
The water absorption of aggregate is determined by measuring the increase in weight of an oven dry sample when immersed in water for 24 hrs. The ratio of the increase in wt to the wt of the dry sample expressed as % is known as absorption of agg.
Agg. absorbs water in concrete & thus affects the workability & final volume of concrete.

## Slide 15
Diagrammatic representation of Moisture in Aggregate